Supporting Information

Magnetically recyclable TiO2/MXene/MnFe2O4 photocatalyst for enhanced peroxymonosulphate-assisted photocatalytic degradation of carbamazepine 
and ibuprofen under simulated solar light

Anna Grzegórska1*, Joseph Chibueze Ofoegbu2, Laura Cervera-Gabalda3, Cristina Gómez-Polo3, Diana Sannino2, Anna Zielińska-Jurek1*

1 Department of Process Engineering and Chemical Technology, Faculty of Chemistry, Gdańsk University of Technology, G. Narutowicza 11/12, 80-233 Gdańsk, Poland

2  Department of Industrial Engineering, University of Salerno, via Giovanni Paolo II, 132, 84084 Fisciano, Italy

3 Departamento de Ciencias-INAMAT2, Universidad Pública de Navarra, Campus de Arrosadia, 31006 Pamplona, Spain

* Corresponding authors: annjurek@pg.edu.pl, anna.grzegorska@pg.edu.pl

- Results and discussion

3.1 Characterization of MnFe2O4, TiO2/Ti3C2 and TiO2/Ti3C2/MnFe2O4 photocatalysts

Table S1. ICP-OES measurements for the  TiO2/Ti3C2/5%MnFe2O4.

| Element | Content (wt%) |
| --- | --- |
| Ti | 33.9930±2.0554 |
| Mn | 0.9436±0.0632 |
| Fe | 2.0062±0.1147 |

Figure S1. SEM area EDS spectrum with atomic and weight percentage of elements.

Figure S2. Survey XPS spectra for TiO2/Ti3C2 composite.

Figure S3. The band gap determination from Kubelka Munk function for various photocatalysts.

Figure S4. HAADF-STEM image and STEM-EDS elemental mapping of TiO2/Ti3C2/5%MnFe2O4.

Figure S5. The Gaussian fitting and deconvolution of PL spectra of the TiO2/Ti3C2 (a), MnFe2O4 (b), and TiO2/Ti3C2/20%MnFe2O4 (c)

Figure S6. CBZ and IBP adsorption (dark reaction) for prepared materials.

Table S2. The rate constant of CBZ and IBP degradation in the CBZ/IBU mixture for selected processes.

| Sample | CBZ degradation rate constant (min-1‧ 10-2) | IBP degradation rate constant (min-1‧ 10-2) |
| --- | --- | --- |
| Photolysis | 0.5±0.02 | 1.2±0.05 |
| Photolysis/PMS | 4.8±0.14 | 5.2±0.23 |
| TiO2/Ti3C2 | 6.9±0.19 | 6.2±0.24 |
| TiO2/Ti3C2/5% MnFe2O4 | 8.9±0.27 | 7.0±0.18 |
| TiO2/Ti3C2/5% MnFe2O4 /PMS (0.25 mM) | 28.6±0.98 | 53.0±1.4 |

Table S3. The TOC removal (%) in the CBZ/IBU mixture for selected processes.

| Sample | TOC removal (%) |
| --- | --- |
| TiO2/Ti3C2/5% MnFe2O4 /PMS (0.25 mM) Amount of photocatalyts - 2g/dm3 | 54±1.7% |
| TiO2/Ti3C2/5% MnFe2O4 /PMS (0.25 mM) Amount of photocatalyts - 1g/dm3 | 51±0.6% |
| TiO2/Ti3C2/5% MnFe2O4 /PMS (0.25 mM) Amount of photocatalyts - 0.5 g/dm3 | 47±1.3% |
| TiO2/Ti3C2/5% MnFe2O4 /PMS (0.25 mM) pH 4.5 | 57±0.8% |
| TiO2/Ti3C2/5% MnFe2O4 /PMS (0.25 mM) pH 9.5 | 43.1±1.1% |
| TiO2/Ti3C2/5% MnFe2O4 /PMS (0.25 mM) Seawater | 60.3±2.1% |

Table S4. The metal lixiviation results for a post-process solution using TiO2/Ti3C2/5% MnFe2O4/PMS (0.25 mM) and amount of photocatalyst – 2 g/dm3.

| Element | ICP-OES (mg/dm3) | Iron Photometric Test (mg/dm3) |
| --- | --- | --- |
| Ti | <LOD | - |
| Mn | 0.423±0.032 | - |
| Fe | 0.089±0.010 | 0.08 |