SUPPORTING INFORMATION

Magnetically-activated 3D printable polylactic acid/polycaprolactone/magnetite composites for magnetic induction heating generation

Itziar Galarreta-Rodriguez1-2*, Alberto Lopez-Ortega1-2*, Eneko Garayo1-2, Juan Jesús Beato-López1-2, Paulo La Roca1-2-3, Vicente Sanchez-Alarcos1-2, Vicente Recarte1-2, Cristina Gómez-Polo1-2 and Jose Ignacio Pérez-Landazábal1-2.

1Departamento de Ciencias, Universidad Pública de Navarra, Campus de Arrosadía, 31006, Pamplona, Spain

2Institute for Advanced Materials and Mathematics (INAMAT2), Universidad Pública de Navarra, Campus de Arrosadía, 31006, Pamplona, Spain

3Centro Atómico Bariloche (CNEA), CONICET, Bariloche 8400, Argentina

*Itziar Galarreta-Rodriguez: itziargalarreta@gmail.com

*Alberto Lopez-Ortega: lopezortega.alberto@gmail.com

Table S1. Weight loss percentages for prepared PLA/PCL and PLA/PCL/MNP filaments.

Fig. S1. AC hysteresis loops of the filaments measured at 311 kHz frequency. SAR values are obtained from the area. The magnetization is normalized by the mass of NPs. The MNP concentration do not affect the AC hysteresis loops.

Fig S2. Commercial iron oxide nanoparticle TEM image (a) and estimated particle size average.

Fig S3. SEM images and corresponding composite EDX maps of the magnetic filament cross section for (a, d) P5%, (b, e) P20%, and (c, f) P60% samples (orange colour in figures d-e corresponds to the Fe absorption edge).

Fig S4. (a) P5% and (b) P20% samples HR-SEM images.

Fig. S5. Thermogravimetry and DTG curves of net PLA and PCL polymers.

| Table S1. Weight loss percentages for prepared PLA/PCL and PLA/PCL/MNP filaments. |
| --- |
|  | PLA | PCL | Rest |
| Composite | % weight | % weight | % weight |
| P0% | 9 | 90 | 1 |
| P5% | 13 | 82 | 5 |
| P10% | 7 | 81 | 12 |
| P20% | 8 | 71 | 21 |
| P40% | 7 | 53 | 40 |
| P60% | 6 | 37 | 57 |

Fig. S1. AC hysteresis loops of the filaments measured at 311 kHz frequency. SAR values are obtained from the area. The magnetization is normalized by the mass of NPs. The MNP concentration do not affect the AC hysteresis loops.

| a) |  | b) |  |
| --- | --- | --- | --- |
| Fig S2. Commercial iron oxide nanoparticle TEM image (a) and estimated particle size average. |

Fig S3. SEM images and corresponding composite EDX maps of the magnetic filament cross section for (a, d) P5%, (b, e) P20%, and (c, f) P60% samples (orange colour in figures d-e corresponds to the Fe absorption edge).

| a) |  | b) |  |
| --- | --- | --- | --- |
| Fig S4. (a) P5% and (b) P20% samples HR-SEM images. |

Fig. S5. Thermogravimetry and DTG curves of net PLA and PCL polymers.