Supplementary Material

Kinetic model formulation (section 2.3)

| dCSiOC2H54dt=- k'h1∙CSiOC2H54∙CH2O | Eq.S1 |
| --- | --- |
| dCSiOC2H53(OH)dt=k'h1∙CSiOC2H54∙CH2O-k'h2∙CSiOC2H53(OH)∙CH2O | Eq.S2 |
| dCSiOC2H52(OH)2dt=k'h2∙CSiOC2H53(OH)∙CH2O-k'h3∙CSiOC2H52(OH)2∙CH2O | Eq.S3 |
| dCSi(OC2H5)(OH)3dt=k'h3∙CSiOC2H52(OH)2∙CH2O-k'h4∙CSi(OC2H5)(OH)3∙CH2O+k'h4KeqCSi(OH)4∙CC2H5OH | Eq.S4 |
| dCSi(OH)4dt=k'h4∙CSiOC2H5OH3∙CH2O-k'h4KeqCSiOH4∙CC2H5OH-2∙k'c1∙CSiOH42-k'c2∙CSiOH4∙C(OH)(SiOR2O)n-SiOH3 | Eq.S5 |
| dCH2Odt=-k'h1∙CSiOC2H54+k'h2∙CSiOC2H53OH+k'h3∙CSiOC2H52OH2+k'h4∙CSiOC2H5OH3∙CH2O +k'h4KeqCSiOH4∙CC2H5OH+k'c1∙CSiOH42+k'c2∙CSiOH4∙C(OH)(SiOR2O)n-SiOH3 | Eq.S6 |
| dCC2H5OHdt=k'h1∙CSiOC2H54+k'h2∙CSiOC2H53OH+k'h3∙CSiOC2H52OH2+k'h4∙CSiOC2H5OH3∙CH2O-k'h4KeqCSiOH4∙CC2H5OH | Eq.S7 |
| C(OH)(SiOR2O)n-SiOH3=CSiOC2H54, 0-CSiOC2H54-x=04CSiOC2H54-xOHx | Eq.S8 |

Fig. S1. Relative concentration of Si(OH)4 and Si(OC2H5)(OH)3 for the reactions at different pH and temperature.

Fig. S2. Relative concentrations of TEOS, hydrolyzed species and the total condensed species at pH 3.8 and 277.2 K, 283.2 K,  293.2 K, and 313.2 K, as a function of (a, c, e, g) reaction time and (b, d, f, h) TEOS conversion. Symbols (, TEOS; , Si(OC2H5)3(OH);  Si(OC2H5)2(OH)2; , Si(OC2H5)(OH)3.  Si(OH)4;   total condensed species) show experimental values and continuous lines show the calculated curves.

Fig. S3. Relative concentrations of TEOS, hydrolyzed species and the total condensed species at pH 4.1 and at 277.2 K, 283.2 K,  293.2 K and 313.2 K as a function of (a, c, e, g) reaction time and (b, d, f, h) TEOS conversion. Symbols (, TEOS; , Si(OC2H5)3(OH);  Si(OC2H5)2(OH)2; , Si(OC2H5)(OH)3.  Si(OH)4;  total condensed species) show experimental values and continuous lines show the calculated curves.

Fig. S4. Relative concentrations of TEOS, hydrolyzed species and the total condensed species at pH 4.4 and at 277.2 K, 283.2 K,  293.2 K and 313.2 K as a function of (a, c, e, g) reaction time and (b, d, f, h) TEOS conversion. Symbols (, TEOS; , Si(OC2H5)3(OH);  Si(OC2H5)2(OH)2; , Si(OC2H5)(OH)3.  Si(OH)4;  total condensed species) show experimental values and continuous lines show the calculated curves.